[image: image1.jpg]wNTECH
ENGINEERED SOLUTIONS



 
12” x 4-1/4” BRIDGE PLANK
SPECIFICATION:  HOT-DIP GALVANIZED STEEL 
Scope:
This specification covers structural quality, light gage, steel bridge plank to be used for structural support or decking on bridges and overpasses.

Material:
Black steel shall meet to the requirements of ASTM A1011, with a minimum yield of 45 ksi. Zinc coating shall conform to ASTM A123, except that the zinc shall be applied at a rate of 2.0 ounces per square foot, total both sides of the planks.
Manufacture:
The planks shall be fabricated with trapezoidal corrugations 12" pitch by 4-1/4" depth and shall be provided with welding slots in the valley of each corrugation when specified. All dimensions are subject to specification and manufacturing tolerances.
Product: 
The nominal physical properties of the steel bridge plank

                           shall conform to the requirements tabulated below.

	
	
	SECTION PROPERTIES

	GAGE
	THICKNESS (in.)
	SECTION MODULUS

(IN^3)PER FT
	MOMENT OF INERTIA

(IN^4)PER FT

	
	
	
	

	9
	0.149
	3.65
	8.62

	8
7
	0.164
0.179
	4.01
4.34
	9.48
10.34



	
	
	
	


Certifications:
Upon request, the manufacturer shall certify that the requirements of this specification have been met.

Installation:

Installation shall be in accordance with the plans and 



specifications, and the manufacturer's recommendations.
Cantilever:        The amount of cantilever (overhang) from the outside bridge  

                          stringer to the end of the plank is a function of the gage and 
                          live loading. Refer to Contech’s “Allowable Cantilever” table 
                          for guidance. 
Reference the project plans for the gage, length, special punching and quantity requirements.
March 2014

