[image: image1.jpg]wNTECH
ENGINEERED SOLUTIONS



 
6” x 2” BRIDGE PLANK
SPECIFICATION – ALUMINIZED STEEL TYPE 2 
Scope:
This specification covers structural quality, light gage, steel bridge plank to be used for structural support or decking on bridges and overpasses.

Material:
Steel shall conform to the requirements of ASTM A929, meeting a minimum yield of 36 ksi. The Aluminized Type 2 coating shall be applied prior to fabrication of the planks at a rate of 1.0 ounce per square foot total both sides.

Manufacture:
The planks shall be fabricated with trapezoidal corrugations 6" pitch by 2" depth and shall be provided with welding slots in the valley of each corrugation when specified. All dimensions are subject to specification and manufacturing tolerances.
Product: 
The nominal physical properties of the steel bridge plank

                           shall conform to the requirements tabulated below.

	
	
	SECTION PROPERTIES

	GAGE
	THICKNESS (in.)
	SECTION MODULUS

(IN^3)PER FT
	MOMENT OF INERTIA

(IN^4)PER FT

	
	
	
	

	
	
	
	

	
	
	
	

	12
	0.105
	1.062
	1.151

	10
	0.135
	1.342
	1.466

	
	
	
	

	
	
	
	


Certifications:
Upon request, the manufacturer shall certify that the requirements of this specification have been met.

Installation:

Installation shall be in accordance with the plans and 



specifications, and the manufacturer's recommendations.
Cantilever:        The amount of cantilever (overhang) from the outside bridge  

                          stringer to the end of the plank is a function of the gage and 
                          live loading. Refer to Contech’s “Allowable Cantilever” table 
                          for guidance. 
Reference the project plans for the gage, length, special punching and quantity requirements.
March 2014

