[image: image1.jpg]wNTECH
ENGINEERED SOLUTIONS



 
9” x 3” BRIDGE PLANK
SPECIFICATION:  HOT-DIP GALVANIZED STEEL 
Scope:
This specification covers structural quality, light gage, steel bridge plank to be used for structural support or decking on bridges and overpasses.

Material:
Black steel in 8, 7, and 5 gage shall meet to the requirements of ASTM A1011, with a minimum yield of 40 ksi. Steel that is          3 gage or heavier shall meet to the requirements of ASTM A1018, with a minimum yield of 40 ksi.  Zinc coating shall conform to ASTM A123 except that the zinc shall be applied at a rate of 2.0 ounces per square foot total both sides.

Manufacture:
The planks shall be fabricated with trapezoidal corrugations 9" pitch by 3" depth and shall be provided with welding slots in the valley of each corrugation when specified. All dimensions are subject to specification and manufacturing tolerances.
Product: 
The nominal physical properties of the steel bridge plank

                           shall conform to the requirements tabulated below.

	
	
	SECTION PROPERTIES

	GAGE
	THICKNESS (in.)
	SECTION MODULUS

(IN^3)PER FT
	MOMENT OF INERTIA

(IN^4)PER FT

	
	
	
	

	8
	0.164
	2.906
	4.680

	7
	0.179
	3.173
	5.120

	5
3
5/16

3/8


	0.209
0.239

0.313

0.375
	3.680
4.160

5.316

6.276
	5.973
6.840

8.751

10.331

	
	
	
	


Certifications:
Upon request, the manufacturer shall certify that the requirements of this specification have been met.

Installation:

Installation shall be in accordance with the plans and 



specifications, and the manufacturer's recommendations.
Cantilever:        The amount of cantilever (overhang) from the outside bridge  

                          stringer to the end of the plank is a function of the gage and 
                          live loading. Refer to Contech’s “Allowable Cantilever” table 
                          for guidance. Reference the project plans for the gage,  

                          length, special punching and quantity requirements.
March 2014

